## Slide 1
1
Plant-wise Defect Analysis
Cut bar length
Dimensional
Toe load
Forging defect
Turning length
Embossing Die Impression / Failure
Others
Marking
Flat Bearing Area
Hardness
AMBE FASTNERS PVT.LTD. Patna Bihar
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
207730 | 1937 | 0.93
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Jan 26 | 0 | 0 | 0.00
Dec 25 | 0 | 0 | 0.00
Sep 25 | 13699 | 39 | 0.28
Aug 25 | 54536 | 651 | 1.19
Jul 25 | 64388 | 706 | 1.10
Jun 25 | 40443 | 324 | 0.80
May 25 | 34664 | 217 | 0.63
Adinath Industries Bhiwadi Haryana
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
2270332 | 12720 | 0.56
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Apr 26 | 85168 | 671 | 0.79
Mar 26 | 131767 | 1012 | 0.77
Feb 26 | 231889 | 1759 | 0.76
Jan 26 | 203101 | 1615 | 0.80
Dec 25 | 284558 | 2232 | 0.78
Nov 25 | 242203 | 1724 | 0.71
Oct 25 | 163413 | 845 | 0.52
Sep 25 | 176936 | 747 | 0.42
Aug 25 | 170675 | 697 | 0.41
Jul 25 | 155705 | 659 | 0.42
Jun 25 | 165193 | 558 | 0.34
May 25 | 137207 | 105 | 0.08

## Slide 2
1
Plant-wise Defect Analysis
Embossing Die Impression / Failure
Dimensional
Cut bar length
Hardness
Marking
Turning length
Others
Turning Bar Diameter
Adinath Industries INC Unit 1 Bhiwadi Haryana
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
2178594 | 11529 | 0.53
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Apr 26 | 80789 | 567 | 0.70
Mar 26 | 79586 | 585 | 0.74
Feb 26 | 74068 | 501 | 0.68
Jan 26 | 438233 | 2578 | 0.59
Dec 25 | 304516 | 1727 | 0.57
Nov 25 | 226436 | 1435 | 0.63
Oct 25 | 203671 | 1214 | 0.60
Sep 25 | 225943 | 1153 | 0.51
Aug 25 | 195440 | 744 | 0.38
Jul 25 | 160472 | 624 | 0.39
Jun 25 | 117846 | 341 | 0.29
May 25 | 71594 | 60 | 0.08
Adinath Industries INC Unit 2 Bhiwadi Haryana
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
309289 | 1991 | 0.64
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Apr 26 | 174072 | 1125 | 0.65
Mar 26 | 135217 | 866 | 0.64

## Slide 3
1
Plant-wise Defect Analysis
Marking
Embossing Die Impression / Failure
Cut bar length
Dimensional
Hardness
Turning length
Others
Avdesh Tracks(P) Ltd. Mohali Punjab
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
1301242 | 8462 | 0.65
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Apr 26 | 53296 | 2223 | 4.17
Mar 26 | 154267 | 844 | 0.55
Feb 26 | 145665 | 763 | 0.52
Jan 26 | 198608 | 1219 | 0.61
Dec 25 | 177753 | 949 | 0.53
Nov 25 | 128620 | 730 | 0.57
Oct 25 | 109358 | 440 | 0.40
Sep 25 | 90677 | 313 | 0.35
Aug 25 | 117392 | 394 | 0.34
Jul 25 | 109402 | 507 | 0.46
Jun 25 | 16204 | 80 | 0.49
Bimla Rail Fasteners Karnal Haryana
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
730104 | 3788 | 0.52
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Feb 26 | 233644 | 1327 | 0.57
Jan 26 | 204540 | 1405 | 0.69
Dec 25 | 110893 | 474 | 0.43
Nov 25 | 31163 | 191 | 0.61
Oct 25 | 15550 | 83 | 0.53
Sep 25 | 127933 | 303 | 0.24
Aug 25 | 6381 | 5 | 0.08

## Slide 4
1
Plant-wise Defect Analysis
Forging defect
Cut bar length
Turning length
Embossing Die Impression / Failure
MPI
Turning Bar Diameter
Others
Dimensional
Bridge Track & Tower Pvt Ltd Raipur Chhatishgarh
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
5146764 | 62805 | 1.22
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Apr 26 | 410802 | 6895 | 1.68
Mar 26 | 351670 | 4938 | 1.40
Feb 26 | 343228 | 4695 | 1.37
Jan 26 | 380851 | 4892 | 1.28
Dec 25 | 548699 | 7233 | 1.32
Nov 25 | 482534 | 6553 | 1.36
Oct 25 | 337924 | 4847 | 1.43
Sep 25 | 697985 | 8387 | 1.20
Aug 25 | 473904 | 5503 | 1.16
Jul 25 | 613766 | 6239 | 1.02
Jun 25 | 225745 | 2016 | 0.89
May 25 | 54808 | 105 | 0.19
CALCUTTA SPRINGS LTD. Howrah West Bengal
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
2635973 | 18279 | 0.69
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Mar 26 | 197928 | 1993 | 1.01
Feb 26 | 256114 | 2206 | 0.86
Jan 26 | 302561 | 2140 | 0.71
Dec 25 | 375049 | 2973 | 0.79
Nov 25 | 318458 | 2646 | 0.83
Oct 25 | 417139 | 2166 | 0.52
Sep 25 | 355915 | 1871 | 0.53
Aug 25 | 198328 | 908 | 0.46
Jul 25 | 113463 | 578 | 0.51
Jun 25 | 85419 | 719 | 0.84
May 25 | 15599 | 79 | 0.51

## Slide 5
1
Plant-wise Defect Analysis
Hardness
Cut bar length
Dimensional
Marking
Embossing Die Impression / Failure
Turning length
Others
Forging defect
MPI
Visual (Sheared Edges, Surface Defects)
Cemcon Railway Industries Gohana Haryana
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
354303 | 3636 | 1.03
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Apr 26 | 67026 | 601 | 0.90
Mar 26 | 32624 | 462 | 1.42
Feb 26 | 40630 | 778 | 1.91
Jan 26 | 23431 | 348 | 1.49
Nov 25 | 50657 | 651 | 1.29
Oct 25 | 40732 | 485 | 1.19
Sep 25 | 0 | 0 | 0.00
Aug 25 | 46504 | 176 | 0.38
Jul 25 | 52699 | 135 | 0.26
Cosmo Enterprise Raipur Chhatishgarh
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
461200 | 3207 | 0.70
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Jan 26 | 0 | 0 | 0.00
Dec 25 | 0 | 0 | 0.00
Jun 25 | 292591 | 2606 | 0.89
May 25 | 168609 | 601 | 0.36

## Slide 6
1
Plant-wise Defect Analysis
Embossing Die Impression / Failure
Dimensional
Hardness
Marking
Cut bar length
Turning length
Others
Forging defect
MPI
Fateh Chand Jain Faridabad Haryana
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
1439148 | 6056 | 0.42
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Apr 26 | 72727 | 458 | 0.63
Mar 26 | 16790 | 120 | 0.71
Feb 26 | 138902 | 1165 | 0.84
Jan 26 | 132743 | 807 | 0.61
Dec 25 | 54772 | 798 | 1.46
Nov 25 | 144113 | 472 | 0.33
Oct 25 | 151718 | 876 | 0.58
Sep 25 | 104320 | 242 | 0.23
Aug 25 | 104777 | 186 | 0.18
Jul 25 | 167505 | 438 | 0.26
Jun 25 | 99053 | 276 | 0.28
May 25 | 94593 | 93 | 0.10
Jee Kay International Track Pvt. Urla Raipur
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
774662 | 9219 | 1.19
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Apr 26 | 267357 | 3405 | 1.27
Mar 26 | 273041 | 3321 | 1.22
Feb 26 | 234264 | 2493 | 1.06

## Slide 7
1
Plant-wise Defect Analysis
Forging defect
Turning Bar Diameter
Dimensional
Turning length
Embossing Die Impression / Failure
Visual (Sheared Edges, Surface Defects)
Others
Cut bar length
MPI
KALIMATA ISPAT (Unit-1) Howrah West Bengal
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
1900765 | 19912 | 1.05
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Apr 26 | 0 | 0 | 0.00
Mar 26 | 26708 | 38 | 0.14
Feb 26 | 275977 | 2388 | 0.87
Jan 26 | 277280 | 2895 | 1.04
Dec 25 | 195702 | 3253 | 1.66
Nov 25 | 218950 | 2497 | 1.14
Oct 25 | 231607 | 2805 | 1.21
Sep 25 | 189733 | 2180 | 1.15
Aug 25 | 298771 | 1571 | 0.53
Jul 25 | 139254 | 1522 | 1.09
Jun 25 | 46783 | 763 | 1.63
KALIMATA ISPAT (Unit-II) Durgapur West Bengal
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
2577961 | 17320 | 0.67
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Apr 26 | 107377 | 469 | 0.44
Mar 26 | 334893 | 2364 | 0.71
Feb 26 | 432347 | 3035 | 0.70
Jan 26 | 453521 | 2760 | 0.61
Dec 25 | 423755 | 3552 | 0.84
Nov 25 | 356696 | 1714 | 0.48
Oct 25 | 313842 | 1568 | 0.50
Sep 25 | 155530 | 1858 | 1.19

## Slide 8
1
Plant-wise Defect Analysis
Other (less weight)
Turning length
Turning Bar Diameter
Forging defect
Cut bar length
Embossing Die Impression / Failure
Others
Dimensional
Flat Bearing Area
Visual (Sheared Edges, Surface Defects)
KALIMATA VYAPAAR (Unit-II) Durgapur West Bengal
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
4172926 | 99939 | 2.39
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Mar 26 | 639221 | 13361 | 2.09
Feb 26 | 473333 | 41508 | 8.77
Jan 26 | 526344 | 8671 | 1.65
Dec 25 | 501848 | 6700 | 1.34
Nov 25 | 421734 | 5508 | 1.31
Oct 25 | 376988 | 7378 | 1.96
Sep 25 | 475451 | 7770 | 1.63
Aug 25 | 500964 | 5874 | 1.17
Jul 25 | 257043 | 3169 | 1.23
KDS ENGG. PVT. LTD. Howrah West Bengal
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
392913 | 4046 | 1.03
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Mar 26 | 85467 | 810 | 0.95
Feb 26 | 148627 | 1471 | 0.99
Jan 26 | 39589 | 323 | 0.82
Dec 25 | 0 | 0 | 0.00
Aug 25 | 38729 | 391 | 1.01
Jul 25 | 49717 | 692 | 1.39
Jun 25 | 30784 | 359 | 1.17

## Slide 9
1
Plant-wise Defect Analysis
Dimensional
Cut bar length
Turning Bar Diameter
Turning length
Forging defect
MPI
Others
Embossing Die Impression / Failure
Flat Bearing Area
KRISHNA INFRATECH Jharsuguda Odisha
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
1896445 | 18130 | 0.96
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Apr 26 | 134973 | 1603 | 1.19
Mar 26 | 42995 | 315 | 0.73
Feb 26 | 95341 | 961 | 1.01
Jan 26 | 131959 | 1159 | 0.88
Dec 25 | 228724 | 2314 | 1.01
Nov 25 | 175431 | 1841 | 1.05
Oct 25 | 155794 | 1514 | 0.97
Sep 25 | 205140 | 1974 | 0.96
Aug 25 | 201251 | 2081 | 1.03
Jul 25 | 280351 | 2784 | 0.99
Jun 25 | 142851 | 1149 | 0.80
May 25 | 101635 | 435 | 0.43
KSE ELECTRICALS PVT LTD Howrah West Bengal
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
5179405 | 45940 | 0.89
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Mar 26 | 680214 | 6085 | 0.89
Feb 26 | 840556 | 7792 | 0.93
Jan 26 | 571012 | 5641 | 0.99
Dec 25 | 641496 | 5866 | 0.91
Nov 25 | 380553 | 3204 | 0.84
Oct 25 | 176257 | 1411 | 0.80
Sep 25 | 335406 | 2507 | 0.75
Aug 25 | 447014 | 4815 | 1.08
Jul 25 | 576522 | 5430 | 0.94
Jun 25 | 276461 | 2564 | 0.93
May 25 | 253914 | 625 | 0.25

## Slide 10
1
Plant-wise Defect Analysis
Dimensional
Turning length
Visual (Sheared Edges, Surface Defects)
Cut bar length
Turning Bar Diameter
Toe load
Others
Embossing Die Impression / Failure
Hardness
MPI
LNVS INFRA PVT. LTD Tatanagar Jharkhand
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
1080103 | 16207 | 1.50
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Mar 26 | 114427 | 1967 | 1.72
Feb 26 | 156270 | 685 | 0.44
Jan 26 | 73944 | 594 | 0.80
Dec 25 | 140773 | 2909 | 2.07
Nov 25 | 124745 | 1682 | 1.35
Oct 25 | 84033 | 4832 | 5.75
Sep 25 | 131555 | 1397 | 1.06
Aug 25 | 103185 | 595 | 0.58
Jul 25 | 72952 | 589 | 0.81
Jun 25 | 16017 | 472 | 2.95
May 25 | 46577 | 405 | 0.87
Apr 25 | 15625 | 80 | 0.51
Lauls Private Ltd. Faridabad Haryana
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
701858 | 1637 | 0.23
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Oct 25 | 47132 | 175 | 0.37
Sep 25 | 110750 | 366 | 0.33
Aug 25 | 101006 | 352 | 0.35
Jul 25 | 115072 | 382 | 0.33
Jun 25 | 104934 | 234 | 0.22
May 25 | 121436 | 79 | 0.07
Apr 25 | 101528 | 49 | 0.05

## Slide 11
1
Plant-wise Defect Analysis
Forging defect
Turning length
Cut bar length
MPI
Turning Bar Diameter
Marking
Others
Embossing Die Impression / Failure
Dimensional
Hardness
M.K.Corporation
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
96807 | 989 | 1.02
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Apr 26 | 33900 | 339 | 1.00
Mar 26 | 28171 | 188 | 0.67
Feb 26 | 34736 | 462 | 1.33
Panna Lal Kanhiya Lal Bansal LLP Sonipat Haryana
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
742210 | 5004 | 0.67
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Apr 26 | 43328 | 634 | 1.46
Feb 26 | 24166 | 147 | 0.61
Jan 26 | 82110 | 790 | 0.96
Dec 25 | 194320 | 1335 | 0.69
Nov 25 | 107018 | 638 | 0.60
Oct 25 | 98912 | 570 | 0.58
Sep 25 | 88768 | 538 | 0.61
Aug 25 | 93116 | 304 | 0.33
Jul 25 | 10472 | 48 | 0.46

## Slide 12
1
Plant-wise Defect Analysis
Turning length
MPI
Forging defect
Cut bar length
Dimensional
Marking
Others
Turning Bar Diameter
Embossing Die Impression / Failure
Pathik Engineering Works Rajnandgaon Chhatishgarh
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
1403246 | 21240 | 1.51
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Mar 26 | 251347 | 3735 | 1.49
Feb 26 | 225613 | 3238 | 1.44
Jan 26 | 149357 | 3112 | 2.08
Dec 25 | 165540 | 1114 | 0.67
Nov 25 | 188288 | 3446 | 1.83
Oct 25 | 157911 | 3584 | 2.27
Sep 25 | 180647 | 2693 | 1.49
Aug 25 | 0 | 0 | 0.00
Jul 25 | 0 | 0 | 0.00
Jun 25 | 0 | 0 | 0.00
May 25 | 84543 | 318 | 0.38
Patil Rail Infrastructure pvt ltd Yellampet, Hyderabad Telangana
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
2633653 | 15154 | 0.58
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Apr 26 | 142298 | 983 | 0.69
Mar 26 | 364147 | 2471 | 0.68
Feb 26 | 264246 | 1501 | 0.57
Jan 26 | 469375 | 1874 | 0.40
Dec 25 | 40345 | 279 | 0.69
Nov 25 | 241285 | 2003 | 0.83
Oct 25 | 228974 | 2159 | 0.94
Sep 25 | 144049 | 1679 | 1.17
Aug 25 | 0 | 0 | 0.00
Jul 25 | 48716 | 820 | 1.68
Jun 25 | 195845 | 891 | 0.45
May 25 | 227475 | 155 | 0.07

## Slide 13
1
Plant-wise Defect Analysis
MPI
Turning length
Cut bar length
Forging defect
Turning Bar Diameter
Visual (Sheared Edges, Surface Defects)
Others
Dimensional
Prakash Metallics Pvt Ltd Raipur Chhatishgarh
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
3133501 | 40477 | 1.29
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Apr 26 | 326870 | 6189 | 1.89
Mar 26 | 305540 | 4412 | 1.44
Feb 26 | 319442 | 4775 | 1.49
Jan 26 | 220523 | 3826 | 1.73
Dec 25 | 348192 | 5607 | 1.61
Nov 25 | 329428 | 4316 | 1.31
Oct 25 | 244796 | 3135 | 1.28
Sep 25 | 303221 | 3318 | 1.09
Aug 25 | 147264 | 1532 | 1.04
Jul 25 | 153192 | 1051 | 0.69
Jun 25 | 86472 | 1306 | 1.51
May 25 | 158127 | 207 | 0.13
Prakash Monomers Pvt Ltd Raipur Chhatishgarh
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
826826 | 5991 | 0.72
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Apr 26 | 215238 | 2325 | 1.08
Mar 26 | 27942 | 504 | 1.80
Jan 26 | 0 | 0 | 0.00
Dec 25 | 0 | 0 | 0.00
Nov 25 | 0 | 0 | 0.00
Oct 25 | 0 | 0 | 0.00
Sep 25 | 0 | 0 | 0.00
Aug 25 | 150277 | 1330 | 0.89
Jul 25 | 47351 | 642 | 1.36
Jun 25 | 0 | 0 | 0.00
May 25 | 241301 | 844 | 0.35
Apr 25 | 144717 | 346 | 0.24

## Slide 14
1
Plant-wise Defect Analysis
Marking
Turning length
Embossing Die Impression / Failure
Cut bar length
Dimensional
Hardness
Others
Turning Bar Diameter
Qualite Steels Sirsa
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
372579 | 1439 | 0.39
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Apr 26 | 102349 | 450 | 0.44
Mar 26 | 72500 | 293 | 0.40
Jan 26 | 146180 | 589 | 0.40
Dec 25 | 51550 | 107 | 0.21
R Rashmi Industries, Jaipur
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
158416 | 719 | 0.45
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Apr 26 | 158416 | 719 | 0.45

## Slide 15
1
Plant-wise Defect Analysis
Cut bar length
Forging defect
Turning length
Marking
Turning Bar Diameter
MPI
Others
Embossing Die Impression / Failure
Dimensional
Royal Infraconstru Raipur Chhatishgarh
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
4082815 | 40977 | 1.00
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Apr 26 | 312134 | 3839 | 1.23
Mar 26 | 570551 | 4219 | 0.74
Feb 26 | 530812 | 5826 | 1.10
Jan 26 | 574850 | 5458 | 0.95
Dec 25 | 692025 | 6607 | 0.95
Nov 25 | 517609 | 5469 | 1.06
Oct 25 | 272990 | 3194 | 1.17
Sep 25 | 273163 | 2876 | 1.05
Aug 25 | 191395 | 1920 | 1.00
Jul 25 | 147286 | 1569 | 1.07
Royal fasteners Raipur Chhatishgarh
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
1102805 | 11564 | 1.05
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Mar 26 | 73292 | 702 | 0.96
Feb 26 | 225801 | 2374 | 1.05
Jan 26 | 135714 | 1525 | 1.12
Dec 25 | 137066 | 1632 | 1.19
Nov 25 | 199442 | 2103 | 1.05
Oct 25 | 84951 | 1178 | 1.39
Sep 25 | 118911 | 1386 | 1.17
Aug 25 | 23623 | 335 | 1.42
Jul 25 | 0 | 0 | 0.00
Jun 25 | 83160 | 276 | 0.33
May 25 | 20845 | 53 | 0.25

## Slide 16
1
Plant-wise Defect Analysis
Forging defect
MPI
Cut bar length
Turning length
Embossing Die Impression / Failure
Dimensional
Others
Turning Bar Diameter
Hardness
Sai Kripa Industries Durg Chhatishgarh
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
785776 | 13765 | 1.75
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Apr 26 | 74513 | 632 | 0.85
Mar 26 | 92316 | 1093 | 1.18
Feb 26 | 57308 | 626 | 1.09
Jan 26 | 59927 | 999 | 1.67
Dec 25 | 104520 | 2415 | 2.31
Nov 25 | 92968 | 2232 | 2.40
Oct 25 | 68771 | 1366 | 1.99
Sep 25 | 33280 | 1195 | 3.59
Aug 25 | 88237 | 1825 | 2.07
Jul 25 | 8698 | 312 | 3.59
Jun 25 | 59471 | 836 | 1.41
May 25 | 19099 | 66 | 0.35
Sheth & Co.
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
528826 | 3988 | 0.75
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Apr 26 | 66072 | 1197 | 1.81
Mar 26 | 163101 | 851 | 0.52
Feb 26 | 93717 | 750 | 0.80
Jan 26 | 157647 | 760 | 0.48
Dec 25 | 48289 | 430 | 0.89

## Slide 17
1
Plant-wise Defect Analysis
Marking
Embossing Die Impression / Failure
Dimensional
Hardness
Cut bar length
Siddartha Metal Fabricators Faridabad Haryana
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
986860 | 6374 | 0.65
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Apr 26 | 160216 | 1089 | 0.68
Mar 26 | 70536 | 450 | 0.64
Feb 26 | 133305 | 896 | 0.67
Jan 26 | 93037 | 867 | 0.93
Dec 25 | 148209 | 1331 | 0.90
Nov 25 | 77638 | 643 | 0.83
Oct 25 | 118323 | 777 | 0.66
Sep 25 | 125428 | 281 | 0.22
Apr 25 | 60168 | 40 | 0.07
Super Steels Mohali Punjab
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
239208 | 634 | 0.27
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Oct 25 | 60342 | 217 | 0.36
Sep 25 | 109376 | 301 | 0.28
Aug 25 | 46850 | 94 | 0.20
Jul 25 | 22640 | 22 | 0.10

## Slide 18
1
Plant-wise Defect Analysis
Forging defect
Turning Bar Diameter
Turning length
Dimensional
Cut bar length
Visual (Sheared Edges, Surface Defects)
Others
Toe load
Surya Alloys Industries Limited Durgapur West Bengal
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
21066131 | 322473 | 1.53
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Apr 26 | 1754068 | 27636 | 1.58
Mar 26 | 221849 | 31038 | 13.99
Feb 26 | 1820686 | 29186 | 1.60
Jan 26 | 1873280 | 30843 | 1.65
Dec 25 | 1867938 | 31339 | 1.68
Nov 25 | 1686431 | 25779 | 1.53
Oct 25 | 1837714 | 26991 | 1.47
Sep 25 | 2114630 | 29048 | 1.37
Aug 25 | 1925013 | 32876 | 1.71
Jul 25 | 2285388 | 32605 | 1.43
Jun 25 | 1534702 | 15102 | 0.98
May 25 | 1220892 | 4280 | 0.35
TECHMA ENGG. Howrah West Bengal
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
273552 | 3221 | 1.18
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Jan 26 | 0 | 0 | 0.00
Dec 25 | 0 | 0 | 0.00
Oct 25 | 52491 | 741 | 1.41
Sep 25 | 121732 | 1217 | 1.00
Aug 25 | 69663 | 678 | 0.97
Jul 25 | 29666 | 585 | 1.97

## Slide 19
1
Plant-wise Defect Analysis
Turning length
Forging defect
Cut bar length
MPI
Turning Bar Diameter
Dimensional
Others
Toe load
Embossing Die Impression / Failure
Technosteel Infraprojects Nagpur Maharastra
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
732640 | 6674 | 0.91
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Mar 26 | 210448 | 1448 | 0.69
Feb 26 | 50964 | 249 | 0.49
Jan 26 | 0 | 0 | 0.00
Dec 25 | 0 | 0 | 0.00
Nov 25 | 5512 | 0 | 0.00
Oct 25 | 233239 | 2447 | 1.05
Sep 25 | 232477 | 2530 | 1.09
UTKARSH INDIA LIMITED Howrah West Bengal
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
1268319 | 16050 | 1.27
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Mar 26 | 73296 | 883 | 1.20
Feb 26 | 123518 | 1589 | 1.29
Jan 26 | 127660 | 1573 | 1.23
Dec 25 | 0 | 0 | 0.00
Nov 25 | 122296 | 5132 | 4.20
Oct 25 | 114287 | 1171 | 1.02
Sep 25 | 187515 | 1359 | 0.72
Aug 25 | 247141 | 1671 | 0.68
Jul 25 | 172632 | 1703 | 0.99
Jun 25 | 83437 | 932 | 1.12
May 25 | 16537 | 37 | 0.22

## Slide 20
1
Plant-wise Defect Analysis
Embossing Die Impression / Failure
Marking
Dimensional
Hardness
Cut bar length
Turning length
Others
Forging defect
MPI
Visual (Sheared Edges, Surface Defects)
Vedkiran Steel Industries Pvt. Ltd. Batala Punjab
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
1438413 | 5925 | 0.41
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Apr 26 | 118811 | 692 | 0.58
Mar 26 | 78686 | 443 | 0.56
Feb 26 | 154454 | 827 | 0.54
Jan 26 | 123402 | 657 | 0.53
Dec 25 | 150503 | 831 | 0.55
Nov 25 | 115784 | 530 | 0.46
Oct 25 | 131433 | 555 | 0.42
Sep 25 | 168616 | 592 | 0.35
Jul 25 | 146597 | 541 | 0.37
Jun 25 | 41934 | 109 | 0.26
May 25 | 184539 | 136 | 0.07
Apr 25 | 23654 | 12 | 0.05
Veera Track Fasteners Rajnandgaon Chhatishgarh
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
775661 | 7656 | 0.99
Month | Inspected (Nos.) | Rejection (Nos.) | % Rej
Mar 26 | 43801 | 464 | 1.06
Jan 26 | 184846 | 2001 | 1.08
Dec 25 | 15416 | 201 | 1.30
Nov 25 | 125347 | 1440 | 1.15
Oct 25 | 52406 | 245 | 0.47
Sep 25 | 169770 | 1334 | 0.79
Aug 25 | 165131 | 1083 | 0.66
Jul 25 | 18944 | 888 | 4.69

## Slide 21
1
Plant-wise Defect Analysis
ERC Inspection – Since April 2025
Cumulative Inspected (Nos.) | Cumulative Rejection (Nos.) | Rejection (%)
78467701 | 897444 | 1.14%
Month | Inspected (Nos.) | Rejected (Nos.) | % Rej
Apr 26 | 4961800 | 64741 | 1.30
Mar 26 | 5944338 | 92275 | 1.55
Feb 26 | 8287363 | 126343 | 1.52
Jan 26 | 8355625 | 91921 | 1.10
Dec 25 | 7952451 | 94208 | 1.18
Nov 25 | 7111339 | 84579 | 1.19
Oct 25 | 6582698 | 78969 | 1.20
Sep 25 | 7768556 | 81454 | 1.05
Aug 25 | 6206567 | 68591 | 1.11
Jul 25 | 6019893 | 65240 | 1.08
Jun 25 | 3745345 | 31913 | 0.85
May 25 | 3273994 | 8900 | 0.27
Apr 25 | 2257732 | 8310 | 0.37

## Slide 22
1
Plant-wise Defect Analysis
Plant-wise Rejection Trend (Rejection > 1%)

## Slide 23
1
Plant-wise Defect Analysis
Top Performing Manufacturers (Lowest Rejection %)

## Slide 24
1
Plant-wise Defect Analysis
Worst Performing Manufacturers (Highest Rejection %)

## Slide 25
1
Plant-wise Defect Analysis
Pareto Analysis for ERC Defects
Highlights: Top defects contribute to ~80% of total rejections, enabling focused process control.

## Slide 26
1
Plant-wise Defect Analysis
Manufacturing Units: High Production Units